Low-Bandgap Nitrides: Issues and Applications

Charles W. Tu

Department of Electrical and Computer Engineering

University of California, San Diego

La Jolla, CA 92093-0407, U.S.A.

ctu@ucsd.edu

Recently there is much interest in III-N-V compound semiconductors, because only a small amount of nitrogen incorporation (less than 5%) in conventional GaAs- and InP-based III-V compounds results in very large bandgap bowing, which is mainly from the downward movement of the conduction band edge.  There are many interesting electronic and optoelectronic applications as well as materials issues.  The latter includes composition fluctuation, decreasing luminescence intensity with increasing nitrogen concentration, band lineup, etc.  Applications include the following.

We demonstrated that InNAsP/GaInAsP single-quantum-well microdisk lasers exhibit a large characteristic temperature, as a result of a large conduction band discontinuity and electron confinement in the quantum well.

An application of more interest is using GaInNAs/GaAs heterostructures on GaAs substrates for 1.3 micron edge-emitting and vertical-cavity surface-emitting lasers (VCSELs), utilizing the well developed GaAs/AlAs distributed Bragg reflectors (DBRs). We have, however, utilized the low-bandgap GaInNAs as the base of a heterojunction bipolar transistor (HBT), which exhibits a 0.4 V reduction in the turn-on voltage for low-power applications.

Besides bandgap bowing, incorporating nitrogen in GaP also results in a change in the band structure.  We have demonstrated that with only 0.5% nitrogen, the Ga(N)P bandgap changes from being indirect to direct, with strong PL emission in the red (650 nm).  We have fabricated light-emitting diodes (LEDs) from GaNP/GaP heterostructures grown with one-step epitaxy, which is simpler than the commercial process of GaAs substrate removal and wafer bonding to a transparent GaP substrate for high-brightness AlInGaP LEDs.  For GaInNP grown on GaAs, we have also shown that the conduction band offset of GaInNP/GaAs can be very small.  Thus, GaInNP could be an ideal material for GaAs-based HBTs.